STEEL AUTHORITY OF INDIA LIMITED

Durgapur Steel Plant — Steel Melting Shop

Data Root Cause Analysis &

Model Enhancement Report

Why Si, S, and P Are Unpredictable — and How to Fix It

| Field | Details |
| --- | --- |
| Prepared by | Siddharth Goutam Kumar, Intern — SAIL DSP |
| Department | Steel Melting Shop (SMS), Durgapur Steel Plant |
| Project | Ferro-Alloy Consumption Optimisation using ML |
| Dataset | 43,334 heats, FY 2023-24 to FY 2025-26 |
| Status | Phase 1 complete (Mn, C) — Phase 2 enhancement proposed |

# 1. Executive Summary

The Phase 1 XGBoost model successfully predicts Manganese (Mn) and Carbon (C) with high accuracy. However, three target variables — Silicon (Si), Sulphur (S), and Phosphorus (P) — show poor predictive performance. This report documents the root cause of each failure through systematic examination of all six raw data files, and presents a concrete path to improvement using features that already exist in the available data but were not included in the initial model.

## Phase 1 Model Results Summary

| Target | R² Score | RMSE | RMSE % of Mean | Status |
| --- | --- | --- | --- | --- |
| Mn | 0.967 | 0.042% | 4.8% | Production Ready |
| C | 0.917 | 0.015% | 7.2% | Production Ready |
| Si | -0.007 | 0.020% | 9.2% | Not Predictable |
| S | 0.110 | 0.006% | 22.4% | Poor |
| P | 0.049 | 0.006% | 21.9% | Not Predictable |

Key finding: Mn and C failures are model problems solved by correct transforms. Si, S, and P failures are data problems — the current 20-feature set simply does not contain the physics that governs these three elements.

# 2. Why Silicon (Si) Is Not Predictable

## 2.1 The Physics of Silicon in Steelmaking

Silicon in the final ladle is controlled by two separate mechanisms: (a) FeSi addition in the ladle, and (b) the grade specification target Si%, which defines how much FeSi the operator adds. The operator does not freely choose FeSi addition — they follow the grade recipe. Therefore, the real explanatory variable for final Si is the grade target specification, not the raw FeSi addition quantity.

## 2.2 What the Data Shows

| Diagnostic | Finding |
| --- | --- |
| Max Pearson r (any feature → Si) | 0.107 (FeSi Into Ladle, across full dataset) |
| FeSi Into Ladle → Si r (train only) | -0.099 (negative! EDA report had wrong sign) |
| Grade_Enc (top feature in Si model) | 12.6% feature importance — highest of all 20 features |
| Si R² with full feature set | -0.007 (worse than predicting the mean) |
| Number of distinct grade Si targets | 70 BOF grades, each with a fixed target Si% in grade spec |

## 2.3 Root Cause

The model cannot predict Si because the grade specification sheet (target Si% per BOF grade) was not included as a feature. The operator adds FeSi to hit the grade spec — so the target Si% IS the primary predictor. Without it, the model sees FeSi quantity (effect) without knowing what Si% it was aiming for (cause).

## 2.4 What Data Can Fix This

| Data Source | File / Sheet | Column Needed | Expected Impact |
| --- | --- | --- | --- |
| Grade specification sheet | Not in current files — request from SMS/QC dept. | Target Si% per BOF grade code | Expected R² jump to 0.70+ |
| Ferro-alloys Consumption (aggregate) | Ferro-alloys_Consumption.xlsx | Grade-wise avg FeSi kg/heat | Moderate — proxy for target Si |

Action required: Request the BOF Grade Chemistry Specification sheet from the SMS Quality Control department. This is a standard document listing target ranges for C, Mn, Si, S, P per grade. It is not in any of the six data files provided.

# 3. Why Sulphur (S) Has Low Accuracy (R² = 0.11)

## 3.1 The Physics of Sulphur Control

Sulphur removal in steelmaking occurs in two stages: (a) hot metal desulphurisation at the blast furnace (pre-BOF), and (b) secondary desulphurisation at the LRF/VAD station after tapping. The final ladle S is therefore determined primarily by the incoming hot metal S (HM_S), the desulphurisation treatment applied, and the slag chemistry during blowing. The current model only has daily-average HM_S — it misses the actual blow-stage slag chemistry.

## 3.2 What the Data Shows

| Diagnostic | Finding |
| --- | --- |
| HM_S → final S correlation | r = 0.559 (moderate) — strongest single predictor |
| Slag analysis coverage in model dataset | 9,476 / 43,334 heats (21.9%) |
| Slag S column in SLAG sheets | Available, 0% null across 12,190 slag rows |
| Slag Basicity (CaO/SiO2) available | Yes — calculated from SLAG-FY23/24/25 sheets |
| BOF Tap S in STEEL sheets | Route '23 1' / '2301': 33,242 unique heats, 0% null |
| Tap S coverage in model dataset | 32,280 / 34,667 train heats (93.1%) |

## 3.3 Root Cause

The model uses only daily-average hot metal S (HM_S), which is a rough proxy. The actual BOF tap S at tapping (before LRF treatment) is available in the STEEL sheets at 93% coverage. Additionally, slag chemistry — specifically CaO/SiO2 basicity and slag S% — directly quantifies the desulphurisation environment during the blow. Neither feature was included in Phase 1.

## 3.4 Enhanced Model Result

Adding BOF Tap S (Tap_S), Slag Basicity, Slag P2O5, and Slag FeO to the feature set — with median imputation for the 78% of heats without slag data — the model already improves substantially:

| Target | Baseline R² | Enhanced R² | Improvement | New Feature Drivers |
| --- | --- | --- | --- | --- |
| S | 0.110 | 0.552 | +0.442 | Tap_S + Slag_Basicity + Slag_S |
| P | 0.049 | 0.597 | +0.548 | Tap_P + Slag_P2O5 + Slag_FeO |
| Si | -0.007 | 0.001 | +0.008 | No improvement — grade spec still missing |

This improvement was achieved using existing data that was available but not used. With full slag coverage (21.9% currently), performance will improve further once blast furnace records are consistently merged.

# 4. Why Phosphorus (P) Has Low Accuracy (R² = 0.049)

## 4.1 The Physics of Phosphorus Control

Phosphorus partition between steel and slag is governed by the Slag Partition Coefficient, which depends on: (a) slag oxidising power (FeO%), (b) slag basicity (CaO/SiO2), (c) bath temperature at tapping (TapTemp), and (d) incoming hot metal P (HM_P). The current model has HM_P as the only P-related input — it is missing all slag variables and tap temperature.

## 4.2 What the Data Shows

| Diagnostic | Finding |
| --- | --- |
| HM_P → final P correlation | r = 0.039 (essentially zero — weakest feature) |
| Slag P2O5 available | Yes — in SLAG-FY23/24/25 sheets, 0% null, 12,190 rows |
| Slag FeO available | Yes — 0% null, range 0% to 75.4% |
| Slag basicity available | Yes — CaO/SiO2 ratio, mean 2.80 |
| BOF Tap P in STEEL sheets | Route '23 1': 33,242 heats, 0% null |
| Tap P coverage in model dataset | 32,280 / 34,667 train heats (93.1%) |
| TapTemp / TapWeight | NOT in PRAVARTANAM ADDITIONS file — source unknown |

## 4.3 Root Cause

P dephosphorisation is a slag-chemistry phenomenon. The current feature set has only HM_P (feed-forward input) but lacks all the slag-side variables that determine P partition. The SLAG sheets have this data (P2O5, FeO, Basicity) at 21.9% heat coverage. The STEEL sheets have BOF tap P at 93% coverage. With these added, enhanced model already reaches R² = 0.597.

Further improvement path: If TapTemp (tapping temperature) can be sourced from BOF Level 2 automation logs, it is one of the strongest P partition predictors and would push R² above 0.70.

# 5. Full Audit of All Six Data Files

## 5.1 File-by-File Findings

| File | Rows | Used in Phase 1? | What It Contains | Usable for Phase 2? |
| --- | --- | --- | --- | --- |
| PRAVARTANAM-ADDITIONS_SMS | 52,732 heats | Yes (primary features) | BOF process inputs: FA additions, O2, lime, scrap. 4 extra columns not used: Coke/PetroCoke/Aluminium/Bauxite Into Ladle, Splashing Lime/Dolomite, O2 Total Reblows. | Yes — add 4 unused columns as features |
| Liquid_Steel_Composition | 51,786 heats | Yes (targets) | Final ladle chemistry: C, Mn, P, S, Si + 22 other elements. MN/S and MN/SI ratios also available. | Already used as targets |
| PRAVARTANAM-HM_ANALYSIS — HM sheets | 26,684 records | Yes (daily avg HM P/S/Si) | Hot metal P, S, Si from 42 blast furnace tapholes. Daily average used. Heat-level not available (no heat number join). | Partial — daily avg is current best |
| PRAVARTANAM-HM_ANALYSIS — SLAG sheets | 12,190 heats | No — excluded Phase 1 | BOF tap slag chemistry: FeO, CaO, SiO2, P2O5, MnO, S, Basicity. 0% nulls. Covers 21.9% of model heats. | Yes — key fix for S and P |
| PRAVARTANAM-HM_ANALYSIS — STEEL sheets | 267,188 rows / 52,702 heats | No — excluded Phase 1 | Multi-stage steel chemistry: Bath (BOF), Ladle Tapping, LRF, VAD, Tundish, Teeming. BOF Tap (route 23) covers 93.1% of model heats with 0% nulls. | Yes — key fix for S and P |
| Bath_Analysis | 52,604 heats | No — excluded Phase 1 | Duplicate of STEEL Bath + Ladle columns. 89.8% null in Bath columns. Ladle columns duplicate Liquid_Steel_Composition targets. | No — redundant, too sparse |
| Ferro-alloys_Consumption | 169 grade-rows (aggregates) | No — trend analysis only | Grade-wise totals for SiMn/FeSi/FeMn, specific consumption (kg/tonne). Not heat-level data — cannot join per heat. | Partial — use as grade-level feature by joining on BOF grade code |
| Grade_wise_Production | 3,061 date-rows | No — trend analysis only | Daily grade production counts and total weight. No chemistry. No heat number join possible. | No — no per-heat information |

# 6. New Features to Add for Phase 2

## 6.1 From STEEL Sheets (BOF Tap Chemistry) — 93% Coverage

Extract Route '23 1' and '2301' rows from STEEL-FY23, STEEL-FY24, STEEL-FY25. These are the first ladle measurement taken at BOF tapping, before any secondary metallurgy treatment.

| New Feature | Source Column | Target(s) It Helps | Why |
| --- | --- | --- | --- |
| Tap_C | C (Route 23) | C, Si | BOF endpoint C = decarburisation completeness |
| Tap_P | P (Route 23) | P | BOF tap P directly feeds final P before LRF treatment |
| Tap_S | S (Route 23) | S | BOF tap S at 93% coverage; far better than daily HM_S proxy |
| Tap_Mn | Mn (Route 23) | Mn | Marginal — confirms FA addition efficiency |

## 6.2 From SLAG Sheets — 21.9% Coverage (Expand by Requesting More Slag Records)

| New Feature | Formula / Source | Target(s) It Helps | Why |
| --- | --- | --- | --- |
| Slag_Basicity | CaO / SiO2 | S, P | Higher basicity = stronger desulphurisation and dephosphorisation |
| Slag_P2O5 | P2O5 column | P | P2O5 in slag directly reflects P removed from steel |
| Slag_FeO | FeO column | P | High FeO = high oxidising power = better P partition |
| Slag_S | S column in slag | S | Slag S% at equilibrium with steel S at tapping |

## 6.3 From PRAVARTANAM-ADDITIONS (Existing File, Unused Columns)

| New Feature | Column Name | Target(s) It Helps | Why |
| --- | --- | --- | --- |
| Coke_Ladle | Coke Into Ladle | C | Carbon addition in ladle — may affect final C |
| PetroCoke_Ladle | Petro Coke Into Ladle | C | Alternative carbon source in ladle |
| Al_Ladle | Aluminium Into Ladle | Si (indirect) | Al deoxidation affects O activity, influences Si equilibrium |
| Splashing_Lime | Splashing Lime | S, P | Post-heat lime splashing affects next heat's slag carryover |
| O2_Total_Reblows | Measered O2 Total Reblows.1 | C, P | Additional O2 during reblows affects decarburisation and dephosphorisation |

## 6.4 Data Still Missing (Not in Any File)

| Missing Feature | Why It Matters | How to Obtain |
| --- | --- | --- |
| Grade target Si% (spec sheet) | PRIMARY driver of final Si — without this, Si model is blind | Request BOF Grade Chemistry Specification from SMS/QC dept. |
| TapTemp (BOF tapping temperature) | Strong P partition predictor (Arrhenius dependency) | Source from BOF Level 2 automation system (BAS/SCADA logs) |
| LRF / VAD treatment time | Secondary metallurgy duration affects S removal | Request from LRF/VAD station process logs |

# 7. Recommended Phase 2 Action Plan

## 7.1 Immediate Actions (This Week)

| # | Action | Data Source | Expected R² Impact |
| --- | --- | --- | --- |
| 1 | Add BOF Tap P, Tap S, Tap C from STEEL sheets (93% coverage) | PRAVARTANAM-HM_ANALYSIS: STEEL-FY23/24/25 | S: 0.11 → 0.55, P: 0.05 → 0.60 |
| 2 | Add Slag Basicity, P2O5, FeO, Slag_S (21.9% coverage, impute missing with median) | PRAVARTANAM-HM_ANALYSIS: SLAG-FY23/24/25 | Incremental on top of #1 |
| 3 | Add 5 unused Additions columns (Coke, PetroCoke, Al, Splashing Lime, O2 Reblows) | PRAVARTANAM-ADDITIONS_SMS.XLSX | Marginal improvement on C |
| 4 | Add grade-level avg FeSi (from Ferro-alloys_Consumption) as a per-grade lookup feature | Ferro-alloys_Consumption.xlsx | Marginal improvement on Si |

## 7.2 Short-Term Actions (Next 2 Weeks)

- Grade Spec: Request BOF Grade Chemistry Specification document from SMS/QC. This single document will be the most impactful addition for Si prediction.

- TapTemp: Request TapTemp from BOF Level 2 system (BAS/SCADA). Tapping temperature is a standard logged parameter in modern BOF systems.

- Slag Coverage: Request expanded slag sampling records. Current 21.9% coverage limits slag feature contribution. Goal: 60%+ coverage.

## 7.3 Expected Final Performance After Phase 2

| Target | Phase 1 R² | Phase 2 R² (Estimated) | Key New Feature |
| --- | --- | --- | --- |
| Mn | 0.967 | ~0.970 | Marginal, already excellent |
| C | 0.917 | ~0.930 | Coke/PetroCoke ladle additions |
| Si | -0.007 | 0.70+ (requires grade spec) | Grade target Si% from spec sheet |
| S | 0.110 | 0.55 (now) → 0.70+ (with LRF time) | Tap_S + Slag_Basicity |
| P | 0.049 | 0.60 (now) → 0.75+ (with TapTemp) | Tap_P + Slag_P2O5 + TapTemp |

# 8. Summary

Three target variables — Si, S, and P — have low predictive accuracy in the Phase 1 model. This report confirms that the root cause is not model architecture but missing features that physically govern these elements:

| Target | Root Cause | Fix Available? | Data Source |
| --- | --- | --- | --- |
| Si | Grade spec target Si% missing from all files | Partial — request grade spec doc | SMS/QC department (not in provided files) |
| S | BOF tap S and slag basicity not included | Yes — in STEEL and SLAG sheets | PRAVARTANAM-HM_ANALYSIS (existing file) |
| P | Tap P, slag P2O5, FeO, TapTemp not included | Partial — Tap_P and slag in existing files; TapTemp from SCADA | PRAVARTANAM-HM_ANALYSIS + BOF Level 2 |

Enhanced model validation (using existing data only, no new requests) already shows:

- S: R² improves from 0.110 to 0.552 (+0.442) by adding BOF tap S and slag chemistry

- P: R² improves from 0.049 to 0.597 (+0.548) by adding BOF tap P, slag P2O5, and FeO

- Si: R² remains at ~0.000 because grade specification data is not in any provided file

Mn (R² = 0.967) and C (R² = 0.917) are production-ready with current features. The Phase 2 enhancements described above will bring S and P to a deployable standard and unlock Si prediction once the grade specification sheet is obtained.

SAIL Durgapur Steel Plant — SMS Internship Project  |  Data analysis phase complete. Phase 2 model training to follow.